SeaTak Technical Specifications Sheet

Adhesive Lap Joint Sheer Strength (ASTM D1002)

All materials with substrate failure (PVC, Soft Wood, Hard Wood, Limestone, and Concrete) indicate that adhesive bond stronger than material.

| Substrate Material | Peak Stress (PSI) | Failure Mode |
| --- | --- | --- |
| Stainless Steel | 914 | Adhesive |
| Cold Rolled Steel | 1,118 | Adhesive/Cohesive |
| Aluminum | 650 | Adhesive |
| Polyvinyl Chloride (PVC) | 526 | Substrate (1) |
| Soft Wood – Pine | 747 | Substrate (2) |
| Hard Wood – Birch | 859 | Substrate (3) |
| Copper | 468 | Adhesive |
| Poly(methyl-methacrylate) – PMMA | 692 | Adhesive |
| Limestone Tile | 325 | Substrate (4) |
| Concrete Tile | 410 | Substrate (4) |

- Substrate (PVC) failed above 500 PSI.  See example picture below:

- Substrate (Soft Wood-Pine) failed above 740 PSI.  See example picture below:

- Substrate (Hard Wood – Birch) failed above 850 PSI.  See picture below:

- Substrate (Limestone) failed above 300 PSI (concrete at 400 PSI).  See picture below: